# Text boxes

Fritsch Particle Sizer 'analysette 22'

Meas.No. 2

Date 29.03.2016

Time 11:14

Operator Kovaleva

ID 7645

Serial No. 123456

29.03.2016 Шунгит ЛП-Ф1

Measuring Range

0.1 [µm]  -  1021.87 [µm]

Pump

70 [%]

Resolution

102 Channels    (20 mm / 385 mm )

Absorption

37.00 [%]

Ultrasonic

On

Measurement Duration

90 [Scans]

Regularization / Modell o_medium

Fraunhofer Calculation selected.

d[4,3] = 0.91µm

Aritmetic Mean = 0.909 µm

Specific Surface Area = 118833.38 cm?/cm?

Elongation ratio of the D50 (0.945 micron) value from last measurement...

Elongation = 6.00

Min.Elongation = 0.00

Max. Elongation = 0.00

Standard Dev. = 0.000

Interpolation Values...     C:\Program Files\a22___32\fritsch\HIMNT_1.FPS

0.050-

1.000µm=

57.09%

1.000-

2.000µm=

42.87%

2.000-

3.000µm=

0.04%

3.000-

4.000µm=

0.00%

4.000-

5.000µm=

0.00%

5.000-

10.000µm=

0.00%

10.000-

20.000µm=

0.00%

20.000-

50.000µm=

0.00%

50.000-

100.000µm=

0.00%

100.000-

200.000µm=

0.00%

Interpolation Values...     C:\Program Files\a22___32\fritsch\10_90.FPV

5.0 %

<=

0.111 µm

10.0 %

<=

0.133 µm

15.0 %

<=

0.605 µm

20.0 %

<=

0.688 µm

25.0 %

<=

0.744 µm

30.0 %

<=

0.790 µm

35.0 %

<=

0.831 µm

40.0 %

<=

0.871 µm

45.0 %

<=

0.908 µm

50.0 %

<=

0.945 µm

55.0 %

<=

0.984 µm

60.0 %

<=

1.023 µm

65.0 %

<=

1.064 µm

70.0 %

<=

1.109 µm

75.0 %

<=

1.154 µm

80.0 %

<=

1.211 µm

85.0 %

<=

1.272 µm

90.0 %

<=

1.355 µm

95.0 %

<=

1.478 µm

99.0 %

<=

1.705 µm